**Blowerproof Liquid Applied Airtight Membranes Specification Clause**

**Description:**

Blowerproof Liquid is a highly flexible, durable and continuous liquid applied airtight membrane. Suitable for direct application onto most construction surfaces without the need for primer. There are two versions, fibre reinforced applied by brush and without fibres to be applied with a roller or spray.

To be applied by a suitably qualified contractor.

**Product reference**

Blowerproof Liquid Brush (*fibre reinforced*) Blowerproof Liquid Roller (*no fibres*)

**Features:**

* Simple and quick to apply
* Changes colour after drying, blue to black, showing when finish can be applied
* Can be plastered over
* Can be used on damp substrates
* Nontoxic, VOC (solvent) free, water soluble

**Indicative coverage:** Between 0.60 and 1.0 kg / m² (about 1.0 mm in thickness) dependent on substrate porosity

**Extensibility:** 380 % (at 0.6 mm dry film thickness)

**Crack bridging**> 2 mm (0.6 mm dry film thickness)

**Diffusion resistance**: 76 854 μ

**Approvals**

British Board of Agrément: Certificate: No 17/5410

**Application**

* Brush
* Roller
* Spray

**UK Supply**

**ENBM Ltd:** [www.blowerproof.co.uk](http://www.blowerproof.co.uk) [info@blowerproof.co.uk](mailto:info@blowerproof.co.uk)

**Product information:** [Technical downloads](http://www.blowerproof.co.uk/technical-data/) Tel: 01793 847 444

**Manufacturer:** Hevadex Bvba.